|  |  |
| --- | --- |
| **Chemical** | **Compatibility** |
|  Acetaldehyde | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Acetamide | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Acetate Solvent | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Acetic Acid | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Acetic Acid 20% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Acetic Acid 80% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Acetic Acid, Glacial | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Acetic Anhydride | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Acetone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetyl Bromide | N/A  |
|  Acetyl Chloride (dry) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Acetylene | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Acrylonitrile | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Adipic Acid | N/A  |
|  Alcohols:Amyl | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Alcohols:Benzyl | N/A  |
|  Alcohols:Butyl | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Alcohols:Diacetone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Alcohols:Ethyl | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Alcohols:Hexyl | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Alcohols:Isobutyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Isopropyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Methyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Octyl | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Alcohols:Propyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Chloride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Aluminum Chloride 20% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Aluminum Fluoride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Aluminum Hydroxide | N/A  |
|  Aluminum Nitrate | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Aluminum Potassium Sulfate 10% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Potassium Sulfate 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alums | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Amines | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ammonia 10% | N/A  |
|  Ammonia Nitrate | N/A  |
|  Ammonia, anhydrous | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Ammonia, liquid | N/A  |
|  Ammonium Acetate | N/A  |
|  Ammonium Bifluoride | N/A  |
|  Ammonium Carbonate | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Ammonium Caseinate | N/A  |
|  Ammonium Chloride | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Ammonium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Nitrate | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Ammonium Oxalate | N/A  |
|  Ammonium Persulfate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ammonium Phosphate, Dibasic | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Phosphate, Monobasic | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Phosphate, Tribasic | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Sulfite | N/A  |
|  Ammonium Thiosulfate | N/A  |
|  Amyl Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Amyl Alcohol | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Amyl Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Aniline | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Aniline Hydrochloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Antifreeze | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Antimony Trichloride | N/A  |
|  Aqua Regia (80% HCl, 20% HNO3) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Arochlor 1248 | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Aromatic Hydrocarbons | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Arsenic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Arsenic Salts | N/A  |
|  Asphalt | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Barium Carbonate | N/A  |
|  Barium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Barium Cyanide | N/A  |
|  Barium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Barium Nitrate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Barium Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Barium Sulfide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Beer | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Beet Sugar Liquids | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Benzaldehyde | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Benzene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Benzene Sulfonic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Benzoic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Benzol | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Benzonitrile | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Benzyl Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Bleaching Liquors | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Borax (Sodium Borate) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Boric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Brewery Slop | N/A  |
|  Bromine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Butadiene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Butane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Butanol (Butyl Alcohol) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Butter | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Buttermilk | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Butyl Amine | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Butyl Ether | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Butyl Phthalate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Butylacetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Butylene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Butyric Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Calcium Bisulfate | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Calcium Bisulfide | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Calcium Bisulfite | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Calcium Carbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Calcium Chlorate | N/A  |
|  Calcium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Calcium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Calcium Hypochlorite | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Calcium Nitrate | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Calcium Oxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Calcium Sulfate | N/A  |
|  Calgon | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Cane Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Carbolic Acid (Phenol) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Carbon Bisulfide | N/A  |
|  Carbon Dioxide (dry) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Carbon Dioxide (wet) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Carbon Disulfide | N/A  |
|  Carbon Monoxide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Carbon Tetrachloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Carbon Tetrachloride (dry) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Carbon Tetrachloride (wet) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Carbonated Water | N/A  |
|  Carbonic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Catsup | N/A  |
|  Chloric Acid | N/A  |
|  Chlorinated Glue | N/A  |
|  Chlorine (dry) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chlorine Water | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chlorine, Anhydrous Liquid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chloroacetic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chlorobenzene (Mono) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chlorobromomethane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chloroform | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chlorosulfonic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chocolate Syrup | N/A  |
|  Chromic Acid 10% | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Chromic Acid 30% | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Chromic Acid 5% | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Chromic Acid 50% | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Chromium Salts | N/A  |
|  Cider | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Citric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Citric Oils | N/A  |
|  Cloroxr (Bleach) | N/A  |
|  Coffee | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Copper Chloride | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Copper Cyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Copper Fluoborate | N/A  |
|  Copper Nitrate | N/A  |
|  Copper Sulfate >5% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Copper Sulfate 5% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Cream | N/A  |
|  Cresols | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Cresylic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Cupric Acid | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Cyanic Acid | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Cyclohexane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Cyclohexanone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Detergents | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Diacetone Alcohol | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Dichlorobenzene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Dichloroethane | N/A  |
|  Diesel Fuel | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Diethyl Ether | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Diethylamine | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Diethylene Glycol | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Dimethyl Aniline | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Dimethyl Formamide | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Diphenyl | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Diphenyl Oxide | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Dyes | N/A  |
|  Epsom Salts (Magnesium Sulfate) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ethane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethanol | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ethanolamine | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ether | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethyl Acetate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ethyl Benzoate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethyl Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethyl Ether | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethyl Sulfate | N/A  |
|  Ethylene Bromide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethylene Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethylene Chlorohydrin | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Ethylene Diamine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ethylene Dichloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethylene Glycol | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ethylene Oxide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Fatty Acids | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Ferric Chloride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ferric Nitrate | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Ferric Sulfate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ferrous Chloride | N/A  |
|  Ferrous Sulfate | N/A  |
|  Fluoboric Acid | N/A  |
|  Fluorine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Fluosilicic Acid | N/A  |
|  Formaldehyde 100% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Formaldehyde 40% | N/A  |
|  Formic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Freon 113 | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Freon 12 | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Freon 22 | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Freon TF | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Freonr 11 | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Fruit Juice | N/A  |
|  Fuel Oils | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Furan Resin | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Furfural | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Gallic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Gasoline (high-aromatic) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Gasoline, leaded, ref. | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Gasoline, unleaded | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Gelatin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Glucose | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Glue, P.V.A. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Glycerin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Glycolic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Gold Monocyanide | N/A  |
|  Grape Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Grease | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Heptane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hexane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Honey | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydraulic Oil (Petro) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydraulic Oil (Synthetic) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrazine | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrobromic Acid 100% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrobromic Acid 20% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrochloric Acid 100% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrochloric Acid 20% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrochloric Acid 37% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrochloric Acid, Dry Gas | N/A  |
|  Hydrocyanic Acid | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Hydrocyanic Acid (Gas 10%) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrofluoric Acid 100% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrofluoric Acid 20% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrofluoric Acid 50% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrofluoric Acid 75% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrofluosilicic Acid 100% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrofluosilicic Acid 20% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrogen Gas | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Hydrogen Peroxide 10% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrogen Peroxide 100% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrogen Peroxide 30% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrogen Peroxide 50% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrogen Sulfide (aqua) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Hydrogen Sulfide (dry) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Hydroquinone | N/A  |
|  Hydroxyacetic Acid 70% | N/A  |
|  Ink | N/A  |
|  Iodine | N/A  |
|  Iodine (in alcohol) | N/A  |
|  Iodoform | N/A  |
|  Isooctane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Isopropyl Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Isopropyl Ether | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Isotane | N/A  |
|  Jet Fuel (JP3, JP4, JP5) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Kerosene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ketones | N/A  |
|  Lacquer Thinners | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Lacquers | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Lactic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Lard | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Latex | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Lead Acetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Lead Nitrate | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Lead Sulfamate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ligroin | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Lime | N/A  |
|  Linoleic Acid | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Lithium Chloride | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Lithium Hydroxide | N/A  |
|  Lubricants | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Lye: Ca(OH)2 Calcium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Lye: KOH Potassium Hydroxide | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Lye: NaOH Sodium Hydroxide | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Magnesium Bisulfate | N/A  |
|  Magnesium Carbonate | N/A  |
|  Magnesium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Magnesium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Magnesium Nitrate | N/A  |
|  Magnesium Oxide | N/A  |
|  Magnesium Sulfate (Epsom Salts) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Maleic Acid | N/A  |
|  Maleic Anhydride | N/A  |
|  Malic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Manganese Sulfate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Mash | N/A  |
|  Mayonnaise | N/A  |
|  Melamine | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Mercuric Chloride (dilute) | N/A  |
|  Mercuric Cyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Mercurous Nitrate | N/A  |
|  Mercury | N/A  |
|  Methane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methanol (Methyl Alcohol) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Methyl Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Acetone | N/A  |
|  Methyl Acrylate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Alcohol 10% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Methyl Bromide | N/A  |
|  Methyl Butyl Ketone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Cellosolve | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Dichloride | N/A  |
|  Methyl Ethyl Ketone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Ethyl Ketone Peroxide | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Methyl Isobutyl Ketone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Isopropyl Ketone | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Methyl Methacrylate | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Methylamine | N/A  |
|  Methylene Chloride | N/A  |
|  Milk | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Mineral Spirits | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Molasses | N/A  |
|  Monochloroacetic acid | N/A  |
|  Monoethanolamine | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Morpholine | N/A  |
|  Motor oil | N/A  |
|  Mustard | N/A  |
|  Naphtha | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Naphthalene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Natural Gas | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nickel Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nickel Nitrate | N/A  |
|  Nickel Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nitrating Acid (<15% HNO3) | N/A  |
|  Nitrating Acid (>15% H2SO4) | N/A  |
|  Nitrating Acid (S1% Acid) | N/A  |
|  Nitrating Acid (S15% H2SO4) | N/A  |
|  Nitric Acid (20%) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitric Acid (50%) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitric Acid (5-10%) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Nitric Acid (Concentrated) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitrobenzene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitrogen Fertilizer | N/A  |
|  Nitromethane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitrous Acid | N/A  |
|  Nitrous Oxide | N/A  |
|  Oils:Aniline | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Anise | N/A  |
|  Oils:Bay | N/A  |
|  Oils:Bone | N/A  |
|  Oils:Castor | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Cinnamon | N/A  |
|  Oils:Citric | N/A  |
|  Oils:Clove | N/A  |
|  Oils:Coconut | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Cod Liver | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Corn | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Cottonseed | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Creosote | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Diesel Fuel (20, 30, 40, 50) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Fuel (1, 2, 3, 5A, 5B, 6) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Oils:Ginger | N/A  |
|  Oils:Hydraulic Oil (Petro) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Hydraulic Oil (Synthetic) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Lemon | N/A  |
|  Oils:Linseed | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Mineral | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Oils:Olive | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Orange | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Palm | N/A  |
|  Oils:Peanut | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Peppermint | N/A  |
|  Oils:Pine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Rapeseed | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Rosin | N/A  |
|  Oils:Sesame Seed | N/A  |
|  Oils:Silicone | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Oils:Soybean | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Sperm (whale) | N/A  |
|  Oils:Tanning | N/A  |
|  Oils:Transformer | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Turbine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oleic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oleum 100% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oleum 25% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oxalic Acid (cold) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ozone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Palmitic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Paraffin | N/A  |
|  Pentane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Perchloric Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Perchloroethylene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Petrolatum | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Petroleum | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Phenol (10%) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Phenol (Carbolic Acid) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Phosphoric Acid (>40%) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Phosphoric Acid (crude) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Phosphoric Acid (molten) | N/A  |
|  Phosphoric Acid (S40%) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Phosphoric Acid Anhydride | N/A  |
|  Phosphorus | N/A  |
|  Phosphorus Trichloride | N/A  |
|  Photographic Developer | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Photographic Solutions | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Phthalic Acid | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Phthalic Anhydride | N/A  |
|  Picric Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Antimony Plating 130°F | N/A  |
|  Plating Solutions,   Arsenic Plating 110°F | N/A  |
|  Plating Solutions,   Brass Plating:     High-Speed Brass Bath 110°F | N/A  |
|  Plating Solutions,   Brass Plating:     Regular Brass Bath 100°F | N/A  |
|  Plating Solutions,   Bronze Plating:     Cu-Cd Bronze Bath R.T. | N/A  |
|  Plating Solutions,   Bronze Plating:     Cu-Sn Bronze Bath 160°F | N/A  |
|  Plating Solutions,   Bronze Plating:     Cu-Zn Bronze Bath 100°F | N/A  |
|  Plating Solutions,   Cadmium Plating:     Cyanide Bath 90°F | N/A  |
|  Plating Solutions,   Cadmium Plating:     Fluoborate Bath 100°F | N/A  |
|  Plating Solutions,   Chromium Plating:     Barrel Chrome Bath 95°F | N/A  |
|  Plating Solutions,   Chromium Plating:     Black Chrome Bath 115°F | N/A  |
|  Plating Solutions,   Chromium Plating:     Chromic-Sulfuric Bath 130°F | N/A  |
|  Plating Solutions,   Chromium Plating:     Fluoride Bath 130°F | N/A  |
|  Plating Solutions,   Chromium Plating:     Fluosilicate Bath 95°F | N/A  |
|  Plating Solutions,   Copper Plating (Acid):     Copper Fluoborate Bath 120°F | N/A  |
|  Plating Solutions,   Copper Plating (Acid):     Copper Sulfate Bath R.T. | N/A  |
|  Plating Solutions,   Copper Plating (Cyanide):     Copper Strike Bath 120°F | N/A  |
|  Plating Solutions,   Copper Plating (Cyanide):     High-Speed Bath 180°F | N/A  |
|  Plating Solutions,   Copper Plating (Cyanide):     Rochelle Salt Bath 150°F | N/A  |
|  Plating Solutions,   Copper Plating (Misc):     Copper (Electroless) | N/A  |
|  Plating Solutions,   Copper Plating (Misc):     Copper Pyrophosphate | N/A  |
|  Plating Solutions,   Gold Plating:     Acid 75°F | N/A  |
|  Plating Solutions,   Gold Plating:     Cyanide 150°F | N/A  |
|  Plating Solutions,   Gold Plating:     Neutral 75°F | N/A  |
|  Plating Solutions,   Indium Sulfamate Plating R.T. | N/A  |
|  Plating Solutions,   Iron Plating:     Ferrous Am Sulfate Bath 150°F | N/A  |
|  Plating Solutions,   Iron Plating:     Ferrous Chloride Bath 190°F | N/A  |
|  Plating Solutions,   Iron Plating:     Ferrous Sulfate Bath 150°F | N/A  |
|  Plating Solutions,   Iron Plating:     Fluoborate Bath 145°F | N/A  |
|  Plating Solutions,   Iron Plating:     Sulfamate 140°F | N/A  |
|  Plating Solutions,   Iron Plating:     Sulfate-Chloride Bath 160°F | N/A  |
|  Plating Solutions,   Lead Fluoborate Plating | N/A  |
|  Plating Solutions,   Nickel Plating:     Electroless 200°F | N/A  |
|  Plating Solutions,   Nickel Plating:     Fluoborate 100-170°F | N/A  |
|  Plating Solutions,   Nickel Plating:     High-Chloride 130-160°F | N/A  |
|  Plating Solutions,   Nickel Plating:     Sulfamate 100-140°F | N/A  |
|  Plating Solutions,   Nickel Plating:     Watts Type 115-160°F | N/A  |
|  Plating Solutions,   Rhodium Plating 120°F | N/A  |
|  Plating Solutions,   Silver Plating 80-120°F | N/A  |
|  Plating Solutions,   Tin-Fluoborate Plating 100°F | N/A  |
|  Plating Solutions,   Tin-Lead Plating 100°F | N/A  |
|  Plating Solutions,   Zinc Plating:     Acid Chloride 140°F | N/A  |
|  Plating Solutions,   Zinc Plating:     Acid Fluoborate Bath R.T. | N/A  |
|  Plating Solutions,   Zinc Plating:     Acid Sulfate Bath 150°F | N/A  |
|  Plating Solutions,   Zinc Plating:     Alkaline Cyanide Bath R.T. | N/A  |
|  Potash (Potassium Carbonate) | N/A  |
|  Potassium Bicarbonate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Bromide | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Chlorate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Potassium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Chromate | N/A  |
|  Potassium Cyanide Solutions | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Dichromate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Ferricyanide | N/A  |
|  Potassium Ferrocyanide | N/A  |
|  Potassium Hydroxide (Caustic Potash) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Potassium Hypochlorite | N/A  |
|  Potassium Iodide | N/A  |
|  Potassium Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Oxalate | N/A  |
|  Potassium Permanganate | N/A  |
|  Potassium Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Sulfide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Propane (liquefied) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Propylene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Propylene Glycol | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Pyridine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Pyrogallic Acid | N/A  |
|  Resorcinal | N/A  |
|  Rosins | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Rum | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Rust Inhibitors | N/A  |
|  Salad Dressings | N/A  |
|  Salicylic Acid | N/A  |
|  Salt Brine (NaCl saturated) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sea Water | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Shellac (Bleached) | N/A  |
|  Shellac (Orange) | N/A  |
|  Silicone | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Silver Bromide | N/A  |
|  Silver Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Soap Solutions | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Soda Ash (see Sodium Carbonate) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sodium Aluminate | N/A  |
|  Sodium Benzoate | N/A  |
|  Sodium Bicarbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Bisulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Bisulfite | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Borate (Borax) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Bromide | N/A  |
|  Sodium Carbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Chlorate | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Sodium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Chromate | N/A  |
|  Sodium Cyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Ferrocyanide | N/A  |
|  Sodium Fluoride | N/A  |
|  Sodium Hydrosulfite | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Sodium Hydroxide (20%) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Hydroxide (50%) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Hydroxide (80%) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Hypochlorite (<20%) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sodium Hypochlorite (100%) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sodium Hyposulfate | N/A  |
|  Sodium Metaphosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Metasilicate | N/A  |
|  Sodium Nitrate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sodium Perborate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sodium Peroxide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sodium Polyphosphate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sodium Silicate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Sulfide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Sulfite | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Tetraborate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Thiosulfate (hypo) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sorghum | N/A  |
|  Soy Sauce | N/A  |
|  Stannic Chloride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Stannic Fluoborate | N/A  |
|  Stannous Chloride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Starch | N/A  |
|  Stearic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Stoddard Solvent | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Styrene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sugar (Liquids) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sulfate (Liquors) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sulfur Chloride | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Sulfur Dioxide | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sulfur Dioxide (dry) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sulfur Hexafluoride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sulfur Trioxide | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sulfur Trioxide (dry) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sulfuric Acid (<10%) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Sulfuric Acid (10-75%) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sulfuric Acid (75-100%) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sulfuric Acid (cold concentrated) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sulfuric Acid (hot concentrated) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sulfurous Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sulfuryl Chloride | N/A  |
|  Tallow | N/A  |
|  Tannic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Tanning Liquors | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Tartaric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Tetrachloroethane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Tetrachloroethylene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Tetrahydrofuran | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Tin Salts | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Toluene (Toluol) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Tomato Juice | N/A  |
|  Trichloroacetic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Trichloroethane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Trichloroethylene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Trichloropropane | N/A  |
|  Tricresylphosphate | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Triethylamine | N/A  |
|  Trisodium Phosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Turpentine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Urea | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Uric Acid | N/A  |
|  Urine | N/A  |
|  Varnish | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Vegetable Juice | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Vinegar | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Vinyl Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Vinyl Chloride | N/A  |
|  Water, Acid, Mine | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Water, Deionized | N/A  |
|  Water, Distilled | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Water, Fresh | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Water, Salt | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Weed Killers | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Whey | N/A  |
|  Whiskey & Wines | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  White Liquor (Pulp Mill) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  White Water (Paper Mill) | N/A  |
|  Xylene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Zinc Chloride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Zinc Hydrosulfite | N/A  |
|  Zinc Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |