|  |  |
| --- | --- |
| **Chemical** | **Compatibility** |
| Acetaldehyde | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetamide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetate Solvent | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetic Acid 20% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetic Acid 80% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetic Acid, Glacial | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetic Anhydride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetyl Bromide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetyl Chloride (dry) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acetylene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Acrylonitrile | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Adipic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Amyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Benzyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Butyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Diacetone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Ethyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Hexyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Isobutyl | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Isopropyl | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Methyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alcohols:Octyl | N/A |
| Alcohols:Propyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aluminum Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aluminum Chloride 20% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aluminum Fluoride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aluminum Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aluminum Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aluminum Potassium Sulfate 10% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aluminum Potassium Sulfate 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aluminum Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Alums | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Amines | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonia 10% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonia Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonia, anhydrous | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonia, liquid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Acetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Bifluoride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Carbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Caseinate | N/A |
| Ammonium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Oxalate | N/A |
| Ammonium Persulfate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Phosphate, Dibasic | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Phosphate, Monobasic | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Phosphate, Tribasic | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Sulfite | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ammonium Thiosulfate | N/A |
| Amyl Acetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Amyl Alcohol | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Amyl Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aniline | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aniline Hydrochloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Antifreeze | N/A |
| Antimony Trichloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aqua Regia (80% HCl, 20% HNO3) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Arochlor 1248 | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Aromatic Hydrocarbons | N/A |
| Arsenic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Arsenic Salts | N/A |
| Asphalt | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Barium Carbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Barium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Barium Cyanide | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Barium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Barium Nitrate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Barium Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Barium Sulfide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Beer | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Beet Sugar Liquids | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Benzaldehyde | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Benzene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Benzene Sulfonic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Benzoic Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Benzol | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Benzonitrile | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Benzyl Chloride | N/A |
| Bleaching Liquors | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Borax (Sodium Borate) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Boric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Brewery Slop | N/A |
| Bromine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butadiene | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butanol (Butyl Alcohol) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butter | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Buttermilk | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butyl Amine | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butyl Ether | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butyl Phthalate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butylacetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butylene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Butyric Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Bisulfate | N/A |
| Calcium Bisulfide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Bisulfite | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Carbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Chlorate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Hypochlorite | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Nitrate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Oxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calcium Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Calgon | N/A |
| Cane Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Carbolic Acid (Phenol) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Carbon Bisulfide | N/A |
| Carbon Dioxide (dry) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Carbon Dioxide (wet) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Carbon Disulfide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Carbon Monoxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Carbon Tetrachloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Carbon Tetrachloride (dry) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Carbon Tetrachloride (wet) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Carbonated Water | N/A |
| Carbonic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Catsup | N/A |
| Chloric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chlorinated Glue | N/A |
| Chlorine (dry) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chlorine Water | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chlorine, Anhydrous Liquid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chloroacetic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chlorobenzene (Mono) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif |
| Chlorobromomethane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chloroform | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chlorosulfonic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chocolate Syrup | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chromic Acid 10% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chromic Acid 30% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chromic Acid 5% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chromic Acid 50% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Chromium Salts | N/A |
| Cider | N/A |
| Citric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Citric Oils | N/A |
| Cloroxr (Bleach) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Coffee | N/A |
| Copper Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Copper Cyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Copper Fluoborate | N/A |
| Copper Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Copper Sulfate >5% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Copper Sulfate 5% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Cream | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Cresols | N/A |
| Cresylic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Cupric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Cyanic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Cyclohexane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Cyclohexanone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Detergents | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Diacetone Alcohol | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Dichlorobenzene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Dichloroethane | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Diesel Fuel | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Diethyl Ether | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Diethylamine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif |
| Diethylene Glycol | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Dimethyl Aniline | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Dimethyl Formamide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Diphenyl | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Diphenyl Oxide | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Dyes | N/A |
| Epsom Salts (Magnesium Sulfate) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethanol | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethanolamine | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ether | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethyl Acetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethyl Benzoate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethyl Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethyl Ether | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethyl Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethylene Bromide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethylene Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethylene Chlorohydrin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethylene Diamine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethylene Dichloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethylene Glycol | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ethylene Oxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Fatty Acids | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ferric Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ferric Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ferric Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ferrous Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ferrous Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Fluoboric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Fluorine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif |
| Fluosilicic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Formaldehyde 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Formaldehyde 40% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Formic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Freon 113 | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Freon 12 | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Freon 22 | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Freon TF | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Freonr 11 | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Fruit Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Fuel Oils | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif |
| Furan Resin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Furfural | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Gallic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif |
| Gasoline (high-aromatic) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif |
| Gasoline, leaded, ref. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Gasoline, unleaded | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Gelatin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Glucose | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Glue, P.V.A. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Glycerin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Glycolic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Gold Monocyanide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif |
| Grape Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Grease | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Heptane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hexane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Honey | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydraulic Oil (Petro) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydraulic Oil (Synthetic) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrazine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrobromic Acid 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrobromic Acid 20% | N/A |
| Hydrochloric Acid 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrochloric Acid 20% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrochloric Acid 37% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrochloric Acid, Dry Gas | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrocyanic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrocyanic Acid (Gas 10%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrofluoric Acid 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrofluoric Acid 20% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrofluoric Acid 50% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrofluoric Acid 75% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrofluosilicic Acid 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrofluosilicic Acid 20% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrogen Gas | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrogen Peroxide 10% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrogen Peroxide 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrogen Peroxide 30% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrogen Peroxide 50% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrogen Sulfide (aqua) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydrogen Sulfide (dry) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydroquinone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Hydroxyacetic Acid 70% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ink | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Iodine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Iodine (in alcohol) | N/A |
| Iodoform | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif |
| Isooctane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Isopropyl Acetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Isopropyl Ether | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Isotane | N/A |
| Jet Fuel (JP3, JP4, JP5) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Kerosene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ketones | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lacquer Thinners | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lacquers | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lactic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lard | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Latex | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lead Acetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lead Nitrate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lead Sulfamate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif |
| Ligroin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lime | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Linoleic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lithium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lithium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lubricants | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lye: Ca(OH)2 Calcium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lye: KOH Potassium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Lye: NaOH Sodium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Magnesium Bisulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Magnesium Carbonate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Magnesium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Magnesium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Magnesium Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Magnesium Oxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Magnesium Sulfate (Epsom Salts) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Maleic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Maleic Anhydride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Malic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Manganese Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Mash | N/A |
| Mayonnaise | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Melamine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Mercuric Chloride (dilute) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Mercuric Cyanide | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif |
| Mercurous Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Mercury | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methanol (Methyl Alcohol) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Acetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Acetone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Acrylate | N/A |
| Methyl Alcohol 10% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Bromide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Butyl Ketone | N/A |
| Methyl Cellosolve | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Dichloride | N/A |
| Methyl Ethyl Ketone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Ethyl Ketone Peroxide | N/A |
| Methyl Isobutyl Ketone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Isopropyl Ketone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methyl Methacrylate | N/A |
| Methylamine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Methylene Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Milk | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Mineral Spirits | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Molasses | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Monochloroacetic acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Monoethanolamine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Morpholine | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Motor oil | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Mustard | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Naphtha | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif |
| Naphthalene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Natural Gas | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nickel Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nickel Nitrate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nickel Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitrating Acid (<15% HNO3) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitrating Acid (>15% H2SO4) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitrating Acid (S1% Acid) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitrating Acid (S15% H2SO4) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitric Acid (20%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitric Acid (50%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitric Acid (5-10%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitric Acid (Concentrated) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitrobenzene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitrogen Fertilizer | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitromethane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitrous Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Nitrous Oxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Aniline | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Anise | N/A |
| Oils:Bay | N/A |
| Oils:Bone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Castor | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Cinnamon | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Citric | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Clove | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Coconut | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Cod Liver | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Corn | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Cottonseed | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Creosote | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Diesel Fuel (20, 30, 40, 50) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Fuel (1, 2, 3, 5A, 5B, 6) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Ginger | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Hydraulic Oil (Petro) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Hydraulic Oil (Synthetic) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Lemon | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Linseed | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Mineral | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Olive | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Orange | N/A |
| Oils:Palm | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Peanut | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Peppermint | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Pine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Rapeseed | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Rosin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Sesame Seed | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Silicone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Soybean | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Sperm (whale) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Tanning | N/A |
| Oils:Transformer | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oils:Turbine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oleic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oleum 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oleum 25% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Oxalic Acid (cold) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Ozone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Palmitic Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Paraffin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Pentane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Perchloric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Perchloroethylene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Petrolatum | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif |
| Petroleum | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Phenol (10%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Phenol (Carbolic Acid) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Phosphoric Acid (>40%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Phosphoric Acid (crude) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Phosphoric Acid (molten) | N/A |
| Phosphoric Acid (S40%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Phosphoric Acid Anhydride | N/A |
| Phosphorus | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Phosphorus Trichloride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Photographic Developer | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Photographic Solutions | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Phthalic Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Phthalic Anhydride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Picric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Antimony Plating 130°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Arsenic Plating 110°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Brass Plating:     High-Speed Brass Bath 110°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Brass Plating:     Regular Brass Bath 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Bronze Plating:     Cu-Cd Bronze Bath R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Bronze Plating:     Cu-Sn Bronze Bath 160°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Bronze Plating:     Cu-Zn Bronze Bath 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Cadmium Plating:     Cyanide Bath 90°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Cadmium Plating:     Fluoborate Bath 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Chromium Plating:     Barrel Chrome Bath 95°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Chromium Plating:     Black Chrome Bath 115°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Chromium Plating:     Chromic-Sulfuric Bath 130°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Chromium Plating:     Fluoride Bath 130°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Chromium Plating:     Fluosilicate Bath 95°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Copper Plating (Acid):     Copper Fluoborate Bath 120°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Copper Plating (Acid):     Copper Sulfate Bath R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Copper Plating (Cyanide):     Copper Strike Bath 120°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Copper Plating (Cyanide):     High-Speed Bath 180°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Copper Plating (Cyanide):     Rochelle Salt Bath 150°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Copper Plating (Misc):     Copper (Electroless) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Copper Plating (Misc):     Copper Pyrophosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Gold Plating:     Acid 75°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Gold Plating:     Cyanide 150°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Gold Plating:     Neutral 75°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Indium Sulfamate Plating R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Iron Plating:     Ferrous Am Sulfate Bath 150°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Iron Plating:     Ferrous Chloride Bath 190°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Iron Plating:     Ferrous Sulfate Bath 150°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Iron Plating:     Fluoborate Bath 145°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Iron Plating:     Sulfamate 140°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Iron Plating:     Sulfate-Chloride Bath 160°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Lead Fluoborate Plating | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Nickel Plating:     Electroless 200°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Nickel Plating:     Fluoborate 100-170°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Nickel Plating:     High-Chloride 130-160°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Nickel Plating:     Sulfamate 100-140°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Nickel Plating:     Watts Type 115-160°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Rhodium Plating 120°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Silver Plating 80-120°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Tin-Fluoborate Plating 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Tin-Lead Plating 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Zinc Plating:     Acid Chloride 140°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Zinc Plating:     Acid Fluoborate Bath R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Zinc Plating:     Acid Sulfate Bath 150°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Plating Solutions,   Zinc Plating:     Alkaline Cyanide Bath R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potash (Potassium Carbonate) | N/A |
| Potassium Bicarbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Bromide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Chlorate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Chromate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Cyanide Solutions | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Dichromate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Ferricyanide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Ferrocyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Hydroxide (Caustic Potash) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Hypochlorite | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Iodide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Oxalate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Permanganate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Potassium Sulfide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Propane (liquefied) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Propylene | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Propylene Glycol | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Pyridine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Pyrogallic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Resorcinal | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Rosins | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Rum | N/A |
| Rust Inhibitors | N/A |
| Salad Dressings | N/A |
| Salicylic Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Salt Brine (NaCl saturated) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sea Water | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Shellac (Bleached) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Shellac (Orange) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Silicone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Silver Bromide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Silver Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Soap Solutions | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Soda Ash (see Sodium Carbonate) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Acetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Aluminate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Benzoate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Bicarbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Bisulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Bisulfite | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Borate (Borax) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Bromide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Carbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Chlorate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Chromate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Cyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Ferrocyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Fluoride | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Hydrosulfite | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Hydroxide (20%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Hydroxide (50%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Hydroxide (80%) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Hypochlorite (<20%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Hypochlorite (100%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Hyposulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Metaphosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Metasilicate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Perborate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Peroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Polyphosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Silicate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Sulfide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Sulfite | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Tetraborate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sodium Thiosulfate (hypo) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sorghum | N/A |
| Soy Sauce | N/A |
| Stannic Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Stannic Fluoborate | N/A |
| Stannous Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Starch | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Stearic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Stoddard Solvent | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Styrene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sugar (Liquids) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfate (Liquors) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfur Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfur Dioxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfur Dioxide (dry) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfur Hexafluoride | N/A |
| Sulfur Trioxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfur Trioxide (dry) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfuric Acid (<10%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfuric Acid (10-75%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfuric Acid (75-100%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfuric Acid (cold concentrated) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfuric Acid (hot concentrated) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfurous Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Sulfuryl Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tallow | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tannic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tanning Liquors | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tartaric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tetrachloroethane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tetrachloroethylene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tetrahydrofuran | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tin Salts | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Toluene (Toluol) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tomato Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Trichloroacetic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Trichloroethane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Trichloroethylene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Trichloropropane | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Tricresylphosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Triethylamine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Trisodium Phosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Turpentine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Urea | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Uric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Urine | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Varnish | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Vegetable Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Vinegar | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Vinyl Acetate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Vinyl Chloride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Water, Acid, Mine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Water, Deionized | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Water, Distilled | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Water, Fresh | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Water, Salt | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Weed Killers | N/A |
| Whey | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Whiskey & Wines | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| White Liquor (Pulp Mill) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| White Water (Paper Mill) | N/A |
| Xylene | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Zinc Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Zinc Hydrosulfite | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |
| Zinc Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif |