|  |  |
| --- | --- |
| **Chemical** | **Compatibility** |
|  Acetaldehyde | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetamide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetate Solvent | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetic Acid 20% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetic Acid 80% | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Acetic Acid, Glacial | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetic Anhydride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetyl Bromide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Acetyl Chloride (dry) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Acetylene | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Acrylonitrile | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Adipic Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Amyl | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Benzyl | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Alcohols:Butyl | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Diacetone | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Alcohols:Ethyl | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Alcohols:Hexyl | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Isobutyl | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Isopropyl | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Methyl | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alcohols:Octyl | N/A  |
|  Alcohols:Propyl | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Chloride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Chloride 20% | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Fluoride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Hydroxide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Nitrate | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Aluminum Potassium Sulfate 10% | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Potassium Sulfate 100% | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aluminum Sulfate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Alums | N/A  |
|  Amines | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ammonia 10% | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ammonia Nitrate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ammonia, anhydrous | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonia, liquid | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Acetate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Bifluoride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Carbonate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Caseinate | N/A  |
|  Ammonium Chloride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Nitrate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Oxalate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Persulfate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Phosphate, Dibasic | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Phosphate, Monobasic | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Phosphate, Tribasic | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Sulfate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Sulfite | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ammonium Thiosulfate | N/A  |
|  Amyl Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Amyl Alcohol | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Amyl Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Aniline | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Aniline Hydrochloride | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Antifreeze | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Antimony Trichloride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Aqua Regia (80% HCl, 20% HNO3) | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Arochlor 1248 | N/A  |
|  Aromatic Hydrocarbons | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Arsenic Acid | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Arsenic Salts | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Asphalt | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Barium Carbonate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Barium Chloride | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Barium Cyanide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Barium Hydroxide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Barium Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Barium Sulfate | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Barium Sulfide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Beer | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Beet Sugar Liquids | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Benzaldehyde | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Benzene | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Benzene Sulfonic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Benzoic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Benzol | N/A  |
|  Benzonitrile | N/A  |
|  Benzyl Chloride | N/A  |
|  Bleaching Liquors | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Borax (Sodium Borate) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Boric Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Brewery Slop | N/A  |
|  Bromine | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Butadiene | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Butane | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Butanol (Butyl Alcohol) | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Butter | N/A  |
|  Buttermilk | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Butyl Amine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Butyl Ether | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Butyl Phthalate | N/A  |
|  Butylacetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Butylene | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Butyric Acid | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Calcium Bisulfate | N/A  |
|  Calcium Bisulfide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Calcium Bisulfite | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Calcium Carbonate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Calcium Chlorate | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Calcium Chloride | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Calcium Hydroxide | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Calcium Hypochlorite | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Calcium Nitrate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Calcium Oxide | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Calcium Sulfate | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Calgon | N/A  |
|  Cane Juice | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Carbolic Acid (Phenol) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Carbon Bisulfide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Carbon Dioxide (dry) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Carbon Dioxide (wet) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Carbon Disulfide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Carbon Monoxide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Carbon Tetrachloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Carbon Tetrachloride (dry) | N/A  |
|  Carbon Tetrachloride (wet) | N/A  |
|  Carbonated Water | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Carbonic Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Catsup | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Chloric Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Chlorinated Glue | N/A  |
|  Chlorine (dry) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chlorine Water | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Chlorine, Anhydrous Liquid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chloroacetic Acid | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Chlorobenzene (Mono) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chlorobromomethane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chloroform | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chlorosulfonic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chocolate Syrup | N/A  |
|  Chromic Acid 10% | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Chromic Acid 30% | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Chromic Acid 5% | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Chromic Acid 50% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Chromium Salts | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Cider | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Citric Acid | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Citric Oils | N/A  |
|  Cloroxr (Bleach) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Coffee | N/A  |
|  Copper Chloride | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Copper Cyanide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Copper Fluoborate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Copper Nitrate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Copper Sulfate >5% | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Copper Sulfate 5% | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Cream | N/A  |
|  Cresols | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Cresylic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Cupric Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Cyanic Acid | N/A  |
|  Cyclohexane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Cyclohexanone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Detergents | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Diacetone Alcohol | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Dichlorobenzene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Dichloroethane | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Diesel Fuel | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Diethyl Ether | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Diethylamine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Diethylene Glycol | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Dimethyl Aniline | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Dimethyl Formamide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Diphenyl | N/A  |
|  Diphenyl Oxide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Dyes | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Epsom Salts (Magnesium Sulfate) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ethane | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ethanol | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Ethanolamine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ether | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethyl Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethyl Benzoate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethyl Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethyl Ether | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethyl Sulfate | N/A  |
|  Ethylene Bromide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethylene Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethylene Chlorohydrin | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethylene Diamine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethylene Dichloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ethylene Glycol | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ethylene Oxide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Fatty Acids | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ferric Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ferric Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ferric Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ferrous Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ferrous Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Fluoboric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Fluorine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Fluosilicic Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Formaldehyde 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Formaldehyde 40% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Formic Acid | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Freon 113 | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Freon 12 | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Freon 22 | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Freon TF | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Freonr 11 | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Fruit Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Fuel Oils | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Furan Resin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Furfural | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Gallic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Gasoline (high-aromatic) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Gasoline, leaded, ref. | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Gasoline, unleaded | C2-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Gelatin | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Glucose | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Glue, P.V.A. | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Glycerin | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Glycolic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Gold Monocyanide | N/A  |
|  Grape Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Grease | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Heptane | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Hexane | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Honey | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydraulic Oil (Petro) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydraulic Oil (Synthetic) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrazine | N/A  |
|  Hydrobromic Acid 100% | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrobromic Acid 20% | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrochloric Acid 100% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Hydrochloric Acid 20% | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrochloric Acid 37% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrochloric Acid, Dry Gas | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrocyanic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrocyanic Acid (Gas 10%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrofluoric Acid 100% | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Hydrofluoric Acid 20% | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrofluoric Acid 50% | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrofluoric Acid 75% | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Hydrofluosilicic Acid 100% | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrofluosilicic Acid 20% | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrogen Gas | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrogen Peroxide 10% | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrogen Peroxide 100% | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrogen Peroxide 30% | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrogen Peroxide 50% | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydrogen Sulfide (aqua) | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydrogen Sulfide (dry) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Hydroquinone | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Hydroxyacetic Acid 70% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Ink | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Iodine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Iodine (in alcohol) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Iodoform | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Isooctane | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Isopropyl Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Isopropyl Ether | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Isotane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Jet Fuel (JP3, JP4, JP5) | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Kerosene | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Ketones | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Lacquer Thinners | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Lacquers | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Lactic Acid | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Lard | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Latex | N/A  |
|  Lead Acetate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Lead Nitrate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Lead Sulfamate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ligroin | N/A  |
|  Lime | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Linoleic Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Lithium Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Lithium Hydroxide | N/A  |
|  Lubricants | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Lye: Ca(OH)2 Calcium Hydroxide | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Lye: KOH Potassium Hydroxide | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Lye: NaOH Sodium Hydroxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Magnesium Bisulfate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Magnesium Carbonate | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Magnesium Chloride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Magnesium Hydroxide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Magnesium Nitrate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Magnesium Oxide | N/A  |
|  Magnesium Sulfate (Epsom Salts) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Maleic Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Maleic Anhydride | N/A  |
|  Malic Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Manganese Sulfate | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Mash | N/A  |
|  Mayonnaise | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Melamine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Mercuric Chloride (dilute) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Mercuric Cyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Mercurous Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Mercury | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Methane | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Methanol (Methyl Alcohol) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Methyl Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Acetone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Acrylate | N/A  |
|  Methyl Alcohol 10% | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Methyl Bromide | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Butyl Ketone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Methyl Cellosolve | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Dichloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Methyl Ethyl Ketone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Ethyl Ketone Peroxide | N/A  |
|  Methyl Isobutyl Ketone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Isopropyl Ketone | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methyl Methacrylate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Methylamine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Methylene Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Milk | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Mineral Spirits | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Molasses | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Monochloroacetic acid | N/A  |
|  Monoethanolamine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Morpholine | N/A  |
|  Motor oil | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Mustard | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Naphtha | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Naphthalene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Natural Gas | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nickel Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nickel Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nickel Sulfate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nitrating Acid (<15% HNO3) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitrating Acid (>15% H2SO4) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitrating Acid (S1% Acid) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitrating Acid (S15% H2SO4) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitric Acid (20%) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nitric Acid (50%) | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Nitric Acid (5-10%) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nitric Acid (Concentrated) | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Nitrobenzene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Nitrogen Fertilizer | N/A  |
|  Nitromethane | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Nitrous Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Nitrous Oxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Aniline | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Anise | N/A  |
|  Oils:Bay | N/A  |
|  Oils:Bone | N/A  |
|  Oils:Castor | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Cinnamon | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Citric | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Clove | N/A  |
|  Oils:Coconut | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Cod Liver | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Corn | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Cottonseed | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Creosote | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Oils:Diesel Fuel (20, 30, 40, 50) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Fuel (1, 2, 3, 5A, 5B, 6) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Ginger | N/A  |
|  Oils:Hydraulic Oil (Petro) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Hydraulic Oil (Synthetic) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Lemon | N/A  |
|  Oils:Linseed | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Mineral | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Olive | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Oils:Orange | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Oils:Palm | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Peanut | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Peppermint | N/A  |
|  Oils:Pine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oils:Rapeseed | N/A  |
|  Oils:Rosin | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Oils:Sesame Seed | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Silicone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Soybean | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oils:Sperm (whale) | N/A  |
|  Oils:Tanning | N/A  |
|  Oils:Transformer | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Oils:Turbine | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Oleic Acid | C2-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Oleum 100% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oleum 25% | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Oxalic Acid (cold) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Ozone | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Palmitic Acid | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Paraffin | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Pentane | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Perchloric Acid | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Perchloroethylene | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Petrolatum | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Petroleum | N/A  |
|  Phenol (10%) | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Phenol (Carbolic Acid) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Phosphoric Acid (>40%) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Phosphoric Acid (crude) | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Phosphoric Acid (molten) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Phosphoric Acid (S40%) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Phosphoric Acid Anhydride | N/A  |
|  Phosphorus | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Phosphorus Trichloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Photographic Developer | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Photographic Solutions | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Phthalic Acid | N/A  |
|  Phthalic Anhydride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Picric Acid | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Antimony Plating 130°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Arsenic Plating 110°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Brass Plating:     High-Speed Brass Bath 110°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Brass Plating:     Regular Brass Bath 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Bronze Plating:     Cu-Cd Bronze Bath R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Bronze Plating:     Cu-Sn Bronze Bath 160°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Bronze Plating:     Cu-Zn Bronze Bath 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Cadmium Plating:     Cyanide Bath 90°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Cadmium Plating:     Fluoborate Bath 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Chromium Plating:     Barrel Chrome Bath 95°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Chromium Plating:     Black Chrome Bath 115°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Chromium Plating:     Chromic-Sulfuric Bath 130°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Chromium Plating:     Fluoride Bath 130°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Chromium Plating:     Fluosilicate Bath 95°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Copper Plating (Acid):     Copper Fluoborate Bath 120°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Copper Plating (Acid):     Copper Sulfate Bath R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Copper Plating (Cyanide):     Copper Strike Bath 120°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Copper Plating (Cyanide):     High-Speed Bath 180°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Copper Plating (Cyanide):     Rochelle Salt Bath 150°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Copper Plating (Misc):     Copper (Electroless) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Copper Plating (Misc):     Copper Pyrophosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Gold Plating:     Acid 75°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Gold Plating:     Cyanide 150°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Gold Plating:     Neutral 75°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Indium Sulfamate Plating R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Iron Plating:     Ferrous Am Sulfate Bath 150°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Iron Plating:     Ferrous Chloride Bath 190°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Iron Plating:     Ferrous Sulfate Bath 150°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Iron Plating:     Fluoborate Bath 145°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Iron Plating:     Sulfamate 140°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Iron Plating:     Sulfate-Chloride Bath 160°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Lead Fluoborate Plating | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Nickel Plating:     Electroless 200°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Nickel Plating:     Fluoborate 100-170°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Nickel Plating:     High-Chloride 130-160°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Nickel Plating:     Sulfamate 100-140°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Nickel Plating:     Watts Type 115-160°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Rhodium Plating 120°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Silver Plating 80-120°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Tin-Fluoborate Plating 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Tin-Lead Plating 100°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Zinc Plating:     Acid Chloride 140°F | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Zinc Plating:     Acid Fluoborate Bath R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Plating Solutions,   Zinc Plating:     Acid Sulfate Bath 150°F | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Plating Solutions,   Zinc Plating:     Alkaline Cyanide Bath R.T. | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potash (Potassium Carbonate) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Bicarbonate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Bromide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Chlorate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Chloride | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Chromate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Cyanide Solutions | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Dichromate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Ferricyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Ferrocyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Hydroxide (Caustic Potash) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Hypochlorite | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Potassium Iodide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Nitrate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Oxalate | N/A  |
|  Potassium Permanganate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Sulfate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Potassium Sulfide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Propane (liquefied) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Propylene | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Propylene Glycol | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Pyridine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Pyrogallic Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Resorcinal | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Rosins | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Rum | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Rust Inhibitors | N/A  |
|  Salad Dressings | N/A  |
|  Salicylic Acid | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Salt Brine (NaCl saturated) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sea Water | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Shellac (Bleached) | N/A  |
|  Shellac (Orange) | N/A  |
|  Silicone | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Silver Bromide | N/A  |
|  Silver Nitrate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Soap Solutions | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Soda Ash (see Sodium Carbonate) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Acetate | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sodium Aluminate | N/A  |
|  Sodium Benzoate | B1-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sodium Bicarbonate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Bisulfate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Bisulfite | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Borate (Borax) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Bromide | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sodium Carbonate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Chlorate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Chloride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Chromate | N/A  |
|  Sodium Cyanide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Ferrocyanide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Fluoride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Hydrosulfite | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Sodium Hydroxide (20%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Hydroxide (50%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Hydroxide (80%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Hypochlorite (<20%) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Hypochlorite (100%) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sodium Hyposulfate | N/A  |
|  Sodium Metaphosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Metasilicate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Nitrate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Perborate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Peroxide | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sodium Polyphosphate | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Silicate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Sulfate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Sulfide | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Sulfite | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Tetraborate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sodium Thiosulfate (hypo) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sorghum | N/A  |
|  Soy Sauce | N/A  |
|  Stannic Chloride | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Stannic Fluoborate | N/A  |
|  Stannous Chloride | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Starch | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Stearic Acid | B2-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Stoddard Solvent | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Styrene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sugar (Liquids) | N/A  |
|  Sulfate (Liquors) | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sulfur Chloride | C1-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Sulfur Dioxide | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sulfur Dioxide (dry) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sulfur Hexafluoride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Sulfur Trioxide | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sulfur Trioxide (dry) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sulfuric Acid (<10%) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sulfuric Acid (10-75%) | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sulfuric Acid (75-100%) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sulfuric Acid (cold concentrated) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sulfuric Acid (hot concentrated) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Sulfurous Acid | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Sulfuryl Chloride | N/A  |
|  Tallow | N/A  |
|  Tannic Acid | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Tanning Liquors | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Tartaric Acid | A1-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Tetrachloroethane | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Tetrachloroethylene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Tetrahydrofuran | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Tin Salts | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Toluene (Toluol) | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Tomato Juice | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Trichloroacetic Acid | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Trichloroethane | C-Fairhttp://www.coleparmer.com/techinfo/images/face-C_17-16.gif  |
|  Trichloroethylene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Trichloropropane | N/A  |
|  Tricresylphosphate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Triethylamine | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Trisodium Phosphate | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Turpentine | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Urea | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Uric Acid | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Urine | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Varnish | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Vegetable Juice | N/A  |
|  Vinegar | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Vinyl Acetate | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Vinyl Chloride | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Water, Acid, Mine | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Water, Deionized | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Water, Distilled | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Water, Fresh | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Water, Salt | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Weed Killers | N/A  |
|  Whey | N/A  |
|  Whiskey & Wines | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  White Liquor (Pulp Mill) | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  White Water (Paper Mill) | A-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |
|  Xylene | D-Severe Effecthttp://www.coleparmer.com/techinfo/images/face-D_17-16.gif  |
|  Zinc Chloride | B-Goodhttp://www.coleparmer.com/techinfo/images/face-B_17-16.gif  |
|  Zinc Hydrosulfite | N/A  |
|  Zinc Sulfate | A2-Excellenthttp://www.coleparmer.com/techinfo/images/face-A_17-15.gif  |